BINA DURACOURT

Acrylic Sports-Court Surfacing System

GUIDE SPECIFICATION & METHOD STATEMENT

Bina Paint Marketing Sdn Bhd (715326-P)  ·  No. 10, Jalan 9/7, Taman IKS Seksyen 9, 43650 Bandar Baru Bangi, Selangor  ·  Tel 03-8926 0012  ·  binapaint.com.my

SIRIM eco-label · MyHIJAU · SPAN registered  |  25+ years · 600+ sports courts delivered

This is an editable guide specification. Consultants/QS may adapt clauses to the specific sport, dimensions, substrate and project requirements. Confirm current product data against the latest Bina Paint TDS/SDS.

# 1. General

## 1.1 Scope

Supply and application of the Bina Duracourt water-based acrylic sports-court surfacing system over a new or existing concrete or bituminous (premix/asphalt) base, including surface preparation, system coats and court line-marking to the relevant federation standard for the nominated sport(s).

## 1.2 System description

A multi-coat acrylic surfacing system comprising a bitumen-emulsion binder coat (Duracourt BE3100) on concrete, acrylic mastic build coats, acrylic colour wearing coats and line-marking. Standard and Cushioned (Pro) build-ups are available. The system is non-skid, non-reflective, UV- and ponding-resistant, and suitable for indoor and outdoor courts.

## 1.3 Manufacturer

Bina Paint Marketing Sdn Bhd. Materials shall be the Bina Duracourt product line or approved equivalent. Manufacturer to provide TDS and SDS on request.

## 1.4 Applicator

Application by a Bina-approved applicator. Bina offers a single design–supply–install package.

## 1.5 References

Relevant federation court-dimension standards (e.g. FIFA/AMF futsal, BWF badminton, FIBA basketball, ITF tennis, IFNA netball, ISTAF sepak takraw, FIVB volleyball).

Bina Duracourt, Duracourt BE3100 (bitumen emulsion) and Bina Primacourt Technical Data Sheets (TDS) and Safety Data Sheets (SDS).

Manufacturer surface-preparation and application instructions.

# 2. Products / Materials

The Duracourt acrylic coats (Mastic and Colour) are single-component, water-based, low-VOC, ammonia-free and non-flammable (suitable for enclosed/indoor halls). The Duracourt BE3100 binder coat is a bitumen emulsion.

| Product | Function | Typical |
| --- | --- | --- |
| Duracourt BE3100 - Bitumen Emulsion | Bitumen-emulsion primer/binder coat locking the system to a concrete substrate | 1 coat (concrete) |
| Duracourt Mastic | Acrylic build/texture coats — level the surface and build grip | 2 coats |
| Duracourt Colour | Water-based acrylic wearing/playing surface; matt, non-skid, non-reflective | 2 coats |
| Acrylic line paint | Court line-marking paint, white / contrast colours | To standard |

Key product data (confirm against current TDS):

| Property | Value |
| --- | --- |
| Duracourt Colour — binder | Single-component water-based acrylic |
| Duracourt Colour — weight solids | 65 ± 2 % |
| Duracourt Colour — coverage | 0.2–0.4 L/m² over 2 coats |
| Duracourt Colour — finish | Matt · non-skid · non-reflective |
| Duracourt Colour — colours | Green, Red, Blue, White |
| Duracourt Colour — pack | 20 kg pail / 200 kg drum |
| Primacourt (acrylic base) — volume solids | 50 ± 3 % |
| Primacourt — coverage | ~8 m²/L @ 50 microns |
| Primacourt — DFT | 100–120 microns |
| Drying (25°C) | Touch dry ~30 min · recoat min 2 hr |

# 3. Substrate Requirements

## 3.1 New concrete

Power-floated or wood-float finish, cured a minimum of 28 days, free of curing compounds, laitance, oil and contaminants, and dry (low residual moisture) before coating.

## 3.2 New bituminous (premix / asphalt)

Typical base build-up: 50 mm premix wearing course over 150 mm crusher run over 50 mm sand blinding on compacted subgrade. Allow new asphalt to cure/oxidise before coating. Duracourt has excellent adhesion to bitumen.

## 3.3 Falls / drainage

Outdoor courts to a planar slope of 1% (1:100) minimum so water sheds freely. No ponding deeper than ~3 mm one hour after wetting; birdbaths to be filled and levelled before colour coats.

## 3.4 Surface tolerance

Finished base flat to ±3 mm under a 3 m straightedge.

# 4. Surface Preparation

Clean and degrease; pressure-wash to remove dirt, laitance and contaminants; allow to dry.

Rout and fill cracks; patch depressions and birdbaths with acrylic patch/mastic; allow to cure.

Concrete substrates: apply one coat of Duracourt BE3100 - Bitumen Emulsion primer/binder. Allow to dry.

Verify falls and surface tolerance before proceeding to build coats.

# 5. System Build-Up

Standard Duracourt build-up (top surface applied last):

A. On a concrete base

| Layer | Material | Coats |
| --- | --- | --- |
| 1 | Duracourt BE3100 - Bitumen Emulsion | 1 coat |
| 2 | Duracourt Mastic | 2 coats |
| 3 | Duracourt Colour | 2 coats |
| 4 | Line marking | To standard |

B. On a premix (asphalt) base

| Layer | Material | Coats |
| --- | --- | --- |
| 1 | Premix wearing course (50 mm) over 150 mm crusher run + 50 mm sand blinding | Base |
| 2 | Duracourt Mastic | 2 coats |
| 3 | Duracourt Colour | 2 coats |
| 4 | Line marking | To standard |

Cushioned (Pro) option: additional resilient acrylic build coats between the base and colour coats for shock absorption and player comfort — recommended for competition and high-traffic courts. Specify "Cushioned" where required.

# 6. Application

Methods: brush, roller or rubber squeegee. For squeegee application the mastic may be blended with clean silica sand and clean water.

Mixing: stir thoroughly before use. On hot, sun-heated surfaces material may be thinned up to 1 part clean water to 4 parts Duracourt by volume.

Conditions: apply only to a clean, dry surface. Do not apply if rain is expected within the recoat window, in temperatures below ~10°C, or in conditions preventing proper film formation.

Recoat: touch dry ~30 minutes; allow a minimum of 2 hours between coats (longer in cool/humid conditions). Each coat must be fully dry before the next.

Apply successive coats at right angles where practicable for an even build.

# 7. Line Marking

Set out court lines to the relevant federation standard for the nominated sport(s). Mask and apply acrylic line paint in white or contrast colour. For multi-sport (multipurpose) courts, colour-code each sport’s lines for clarity.

# 8. Curing & Opening to Play

Allow each coat to dry as specified. Permit light foot traffic only after the final coat is dry; open to full play after the system has cured. Where constructed on new concrete, allow the concrete to cure 14 days minimum (28 days recommended) before play.

# 9. Quality Assurance — Inspection Hold Points

| Hold point | Check |
| --- | --- |
| H1 | Substrate acceptance — cure, moisture, falls (1%), tolerance, cleanliness |
| H2 | Primer / binder coat acceptance (concrete) |
| H3 | Build (mastic) and colour coat coverage checks |
| H4 | Line-marking setting-out approval |
| H5 | Final handover inspection |

# 10. Environmental & Safety

Water-based, low-VOC, ammonia-free; SIRIM eco-label / MyHIJAU.

Non-flammable — suitable for enclosed and indoor halls where solvent-based coatings are not permitted.

Refer to product Safety Data Sheets (SDS) for handling, storage and PPE.

# 11. Warranty

System warranty provided by Bina Paint / the approved applicator on a per-project basis, subject to correct substrate, preparation, application and maintenance. Confirm warranty terms with Bina Paint for the specific project.

# 12. Maintenance

Routine cleaning and periodic inspection extend service life. Typical recoat/resurface cycle is approximately 5–8 years depending on usage and exposure. Refer to Bina Duracourt maintenance guidance.

# 13. Specification Support

Bina Paint — Tel/WhatsApp 03-8926 0012 · binapaint.com.my. Request current TDS, SDS, colour samples, court dimension diagrams and project-specific specification support.

Document: Bina Duracourt Guide Specification & Method Statement (editable). Issued by Bina Paint Marketing Sdn Bhd. Verify against the latest manufacturer data before tender issue.